PARAGON BUILDING PRODUCTS

PRODUCT INFORMATION – ITEM #35950

SALTILLO GROUT 2 1/2:1

SALTILLO GROUT: is a precise blend of Portland Cement, aggregate, polymer and colorfast pigment formulated to be used in 1/2” up to 1 ½” wide and deep grout joints.

FEATURES AND BENEFITS:

- Interior or Exterior

- Crack Resistant

- Mexican Tiles, Pavers and Stones

- Requires only the addition of water

- Maximum strength, hardness and durability

PREPARATION: Before grouting, wait 24 hours after the tile has set to insure maximum bond of the tile to surface. If tile is porous, use grout release to aid in cleanup.

CAUTION: In hot weather, prevention of extreme water dehydration is suggested. All cement based products have the potential for efforescence and this is not a defect in manufacturing.

MIXING: Mix entire content of  Saltillo Grout Mix with approximately 1 gallon of cool, clean water. Mix to a usable consistancy, making sure there are no streaks and the color is uinform. Mix with a paddle that will not entrain air into the grout mix, and use a power mixer at 300 RPM or less. Let material stand for 10 to 15 minutes and remix prior to grouting. Do not add additional water after slaking. In cold weather, the powder and water must be above 60 degree Ferenheit

APPLICATION: Spread Saltillo Grout over the face of the tile with a soft rubber grout float. Work the grout back and forth to insure complete filling of the joints. Remove excess grout off the face of the tile using the edge of the rubber float, moving diagonally across the face of the tile. If using grout bag, concult its manufacturer for suitabllity.

CLEANING: Clean excess grout from the surface of the tile as soon as possible without damaging the joints. Use a damp square edged synthetic sponge wiping diagnally cross the joints and clean the sponge often for better results.

CURING: Saltillo Grout Mix becomes firm overnight or faster in hot weather, but does not cure to its full hardness for seven days. For maximum durability dampen joints each day for three days after installation. In tempatures of 90 degree Ferenheit or above, moist curing is needed to prevent rapid dehydration which will cause cracking and powdering. In cold weather  protect the installation from temperatures below 40 degree Ferenheit for at least 24 hours.

Packaging: 50lb. / 22.68 kgs multi-ply 56 /pallet 2,800 lb.

YIELD: A 50 lb sack (22.68 kgs) will yield approximately 50 to 60 square feet with a 1” joint.

LIMITATIONS:

- DO NOT apply when the air or substrate temperature is below 40° F within 24 hours of application.

- DO NOT over water

- DO NOT over mix

- DO NOT apply over substrates that are frozen or contain frost.

- DO NOT use dirty water or tools.

- DO NOT add or mix any materials with this product unless approved by PARAGON CONCRETE PRODUCTS INC.

- DO NOT accelerate cure with fans.

PARAGON BUILDING PRODUCTS

PRODUCT INFORMATION

SALTILLO GROUT 2 1/2:1

TECHNICAL SERVICE:

For, application procedures or surface conditions not specified in literature contact:

Paragon Concrete Products Inc.

2305 S Roof Tile Rd

Casa Grande, AZ 85193

Phone: 520-836-6454

Fax: 520-421-1172

Avoid hazards by following all precautions found in the MSDS (Material Safety Data Sheet), product labels and product information sheets. Please read this information prior to using the product. MSDS are available through

technical service at 520-836-6454.

CAUTION: Contains Portland Cement. Cement causes skin irritations, may cause allergic reactions. Avoid eye contact or prolonged contact with skin. Use of a dust respirator, safety goggles and rubber gloves are recommended. Wash self thoroughly after any contact. In case of eye contact, flush immediately with plenty of water for at least 15 minutes. Consult a physician immediately.

KEEP OUT OF REACH OF CHILDREN

Avoid hazards by following all precautions found in the MSDS (Material Safetl Data Sheet), product labels and product information sheets. Please read this information prior to using the product.

LIMITED WARRANTY:

Paragon Building Products, Inc. (Paragon) warrants that this product and the materials used therin meet or exceed the applicable ASTM standards listed and in force at the time of manufacture. Paragon will replace any product or part which proves defective due to quality of ingrwedients used od due to the manufacturing process itself. This warranty shall apply only if the product is used in stict accordance to applicalbe specifications and instructions provided by Paragon for its use, and Paragon shall not be liable otherwise, Replacement of any defective product or, at Paragon’s option, refund of the purchase price of any defective product shall be the buyers sole remedy under this warranty, and Paragon shall in no event be liable for any damages in excess of the purchase price of the defective product. PARAGON SHALL IN NO EVENT BE LIABLE FOR ANY CONSEQUENTIAL INCIDENTAL  OR SPECIAL DAMMAGES.

This Warranty constitutes the sole warranty given by Paragon in connection with this product, and Paragon has authorized no person to make or give any other warranties or representations, oral or written on its behalf. IN PARTICULAR, THER ARE NO IMPLIED WARRANTIES, INCLUDING WITHOUT EXCEPTION WARRANTIES OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR PURPOSE. No modifications of this warranty in favor of any buyer shall be vaid unless given in writing and signed by an officer of Paragon.

Revised March 2013 r.radel / a.g.